RMG Trolley Repair Process Procedures

Introduction

IST Engineering S.A has been requested by Piraeus Port Authority S.A. to issue explanatory procedures regarding the repair process for the Trolley Bogie (Figure 1) of Rail Mounted Gantry Cranes (RMG), which are operating at the port of Piraeus Container Terminal I.

Figure 1  Trolley Bogie

Please, refer to the below figure No.2 which indicates the “Trolley Bogie, Wheel Fixing” and the “Bearing Hub” of the trolley bogie.

Bearing “Hub”/Mounting Part

Wheel Fixing

Interface to Transverse Girder

Trolley Bogie Body

Figure 2 Trolley Bogie & Wheel Fixing existing structure

Issued by:

Date: 22. January 2021

Anastasios Adamopoulos I.S.T. S.A.

Dipl. Mechanical Engineer

Approvals and version history

| REVISION | DATE | DESCRIPTION OF CHANGE | APPROVED BY |
| --- | --- | --- | --- |
| A | 05/01/2021 | Preliminary version | Adamopoulos An. |
| B | 22/01/2021 | Final version | Adamopoulos An. |

Context

Abstract	3

Safety specification:	8

2nd Step–Repair Process.	9

3rd Step – Holes creation to the Trolley.	10

4th Step - Structural Reinforcements Welding	10

5th Step. Assembly wheels with Shaft & Reinforcement Rings	14

6th Step. Wheels alignment.	16

Annex A	16

1.	SURFACE PREPARATION	16

2.	PAINTING PROCESS	17

Table 1 Tightening torques	18

3.	ASSEMBLY DRAWINGS	18

Abstract

The scope of this document is to describe all actions, works and repair process for the “Trolley Bogie and Wheel Fixing” reinforcement.

All the welded stiffeners presented in the modified design are used to reinforce the failing welded areas, presented in the below Figure No. 3

| Figure 3. Visual Inspection of the Trolley Bogie Structure |  |
| --- | --- |

From the results which are presented in the study for the’’ Repair Trolley Calculation’’, the following structural reinforcement recommendations apply:

- Reinforcement rings, located at the interior side of each trolley bogie plate that will deliver the bending moment and shear force induced by Fx, Fy and Fz, as indicated in 4, 5 and Figure 6.

- Vertical and horizontal stiffeners (15mm thickness) on both outer sides of the trolley bogie body, as indicated in Figure 4 and Figure 5.

.

- Vertical brackets between the guide roller interface plate and the wheel fixing plate of the trolley body, as indicated in 5 and Figure 6.

- Horizontal inner body brackets, as indicated in Figure 7.

- Horizontal inner body stiffeners, as indicated in Figure 8.

| Proposals: Structure after modification with the Additional Reinforcement – Rings and Stiffeners Reinforcement rings (20mm Thick.) Outer Body Stiffeners (15mm Thick.) Figure 4 Outer body stiffeners (-Y) and reinforcement rings | Reinforcement rings (20mm Thick.) Guide Roller Interface - Brackets (15mm Thick.) Outer Body Stiffeners (15mm Thick.) Figure 5 Outer body stiffeners (+Y), guide roller interface brackets and reinforcement rings |
| --- | --- |
| Reinforcement rings (20mm Thick.) Guide Roller Interface - Brackets (15mm Thick.) Figure 6 Guide roller interface brackets and reinforcement rings | Inner Body Brackets (15mm Thick.) Figure 7 Inner body brackets |

Inner Body Stiffeners (15mm Thick.)

Figure 8. Inner body stiffeners

Safety specification:

Following the Greek Safety Legislation only qualified-certified, trained, and designated person may carry out the repairs.

Note:  The welding operations must be carried out by certified personnel and the NDT (Non Destructive Tests) by a qualified company and certified by the Hellenic Accreditation System (ESYD).

1st Step – Disassembly of Trolley shaft with wheels.

Please follow the below disassembly process:

- Place the Trolley at the parking position.

- Disconnect the power cables of the motors.

- Remove the gear reducer, electrical motor and breaks.

- Remove the safety devices.

- Use the service crane for the elevation and remove the parts.

- Place a hydraulic jack under the lowest point of the trolley at the desirable side.

- Move the shaft with the wheels along the rail.

- Remove the unit with the service crane.

2nd Step–Repair Process.

The second step must be the repair of failure areas by welding along the length of the cracks.

Carry out the MT inspection around the cracks to ensure that the full extent of the crack is detected. After MT completed you can proceed with the repair works.

Plate Cracks Repairing Procedures

- Grinding the painting near the welding cracks rough area, and confirming the exact area of the cracks by MT.

- Grinding the cracks on the welding line and probably existing on the parent metal until the cracks are all cleaned.

- Repair the crack of the welding line according to the OEM original drawing No.12834-5103 (See Fig.9).

Figure 9

- After welding completed, grind the surface smoothly and carry out MT to ensure that the welds are free of defects such as under cuts, porosities and crater cracks etc. Repair if any defects are found out.

- Damaged paint works to be repaired after drilling the holes (See 3rd Step )as follows:

- Power tool cleaning to remove rust.

- For the surface preparation and coating procedure please refers to annex point1&2

table 1.

3rd Step – Holes creation to the Trolley.

Before creating the holes to the Trolley we must temporary reassembly the wheel fixing clampers at the position imposed by the OEM (see Drawing N. 12834-5103) with the Bearing Support (see OEM Drawing N. 12834-5601).

Note: In order to keep the clearance of 2mm between the Trolley body and the clampers we propose to manufacture and insert metal spacers of 2mm thickness (see below Figure No.10).

Figure 10. Clampers assembly using the metal spacer of 2mm for holes creation.

After we can drill the holes of Ø 18,5 H14  according to I.S.T S.A. manufacturing drawing No.A210-5103 (See Annex Figure. 18 ) to the Trolley body and the clampers Coupled.

After drilling, all holes must be cleaned and paint according to instructions (see Annex point 1&2

table 1) at the final stage of repair process.

4th Step - Structural Reinforcements Welding

Make sure that all the necessary parts are available for the repair. (See IST BOM Referring IST SA assembly Drawings IST-A200-5103).

The sequence for the assembly & welding of the Structural Reinforcements is the following:

- Welding of the ‘’Inner  body stiffeners’’ as the instructions below

4

5

3

1

2

6

Welding Inner Body Stiffeners 2,4,5,6,             from bottom side

Welding Inner Body Stiffeners 1,3             on both sides

Figure 11. Inner body brackets welding

| Welding Sequence | BOM Position | DWR No. | Description | Quantity |
| --- | --- | --- | --- | --- |
| 1 | 32 | IST-P232-5103 | INNER STIFFENER 3 | 1 pcs |
| 2 | 31 | IST-P231-5103 | INNER STIFFENER 2 | 1 pcs |
| 3 | 33 | IST-P233-5103 | INNER STIFFENER 4 | 1 pcs |
| 4 | 34 | IST-P234-5103 | INNER STIFFENER 5 | 2 pcs |
| 5 | 35 | IST-P235-5103 | INNER STIFFENER 6 | 2 pcs |
| 6 | 30 | IST-P230-5103 | INNER STIFFENER 1 | 1 pcs |

- Welding of the ‘’Inner body brackets’’ on both sides.

Inner Body Brackets (15mm Thick.)

Figure 12. Inner body brackets welding

- Welding of ‘’Bottom Brackets’’ on both sides

Horizontal Bottom Brackets (15mm) Thick.)

Figure 13. Horizontal Bottom Bracket Outside View (-Y)

Guide Roller Interface - Brackets (15mm Thick.)

Welding of guide roller interface brackets on both sides.

Figure 14.  Roller interface brackets on both sides

- Welding of Outer body stiffeners on both sides.

| Outer Body Stiffeners (15mm Thick.) Figure 15. Outer body stiffeners (-Y) Outside View | Outer Body Stiffeners (15mm Thick.) Figure 16. Outer body stiffeners (+Y), Inside View |
| --- | --- |

Please pay attention to the following points after the Welding Procedures:

- Carry out the MT inspection around the welding areas to ensure that everything is correct. After MT completed you can proceed with the surface treatment and painting.

- For the Surface Treatment please refer to Annex point 1.

- For the coating procedure please refer to annex point 2 and table 1.

5th Step. Assembly wheels with Shaft & Reinforcement Rings

In case it does not need to replace the bearings, ring seals and supports you must follow the below mention actions.

Place the bearing support into the bogie’s housing with small adjusting movements.

Check if the threads and the bolds M20 8.8 are in a proper condition. If not, proceed with the replacement of the bolts.

Place and screw the clampers with the two M20 8.8 bolts (Note: without the metal spacers of 2mm).

Figure 17. Inner Reinforcement Rings Assembly.

Repeat the above mention procedure for rest of the wheels of the trolley.

Notes:

1. Respect the clearance of 2mm as indicated on Drawing N. 12834-1110.

2. Tight with a torque wrench the bolts M20 8.8 with a torque of 410 Nm.

(Assumption: Friction Coefficient 0,14).

Place the reinforcement rings and screw the M16 x 55 DIN 933 8.8 (Hot Deep Galvanized) bolts using spring lock washers M16 DIN 127 (Hot Deep Galvanized)   .

Apply to the bolts M16 8.8 with a torque wrench a torque of 210 Nm

(Assumption: Friction Coefficient 0,14).

(See Appendix Table 2)  Tightening Forces in Nm According to:

EN 13001-3-1:2012+a2:2018 Cranes General Design Part3-1: Limit States and proof competence of steel structure.

6th Step. Wheels alignment.

Following bogies assemblies please proceed with the wheels alignment according to FEM 1.001 3rd edition.

Deliverables to PPA after the completion of the repair works for each RMG.

- ALL certificates from the supplier of the Steel Plates, welding materials and steel parts for each RMG separately.

- Welder’s certificate in force.

- ALL results from NDT’s for each RMG separately.

- Measurements of Trolley wheels.

Annex A

- SURFACE PREPARATION

The painting of the main steel structure will be executed after all oils, humidity and residues have  previously been removed, and after it has been subjected to SA 2 ½ sandblasting according to Swedish regulations SIS 055900 or ISO 8501-1/1998, in accordance with the paint manufactures recommendations. Where shot blasting is not practical, chipping, hammering, scrapping and wire brushing may be employed subject to approval of PPA. Oils and greases shall be removed by suitable solvents.

The following systems shall be adopted:

- Washing (water cleaning);

- Mechanical or manual preparation;

- Preparation by sandblasting.

- PAINTING PROCESS

| Paint type | Dry film thickness (microns) | Number of coats | Colour |
| --- | --- | --- | --- |
| First coat: Zinc epoxy primer | 65 | 1 |  |
| Second coat: Epoxy primer | 60 | 1 |  |
| Third coat: Epoxy primer | 60 | 1 |  |
| Fourth coat: Polyurethane, semigloss | 60 | 1 | RAL 2000 (orange) |
| Total cycle thickness | 245 |  |  |

Table 1. Painting coating specifications

- Tightening torques

Table 2. EN 13001-3-1:2012+a2:2018 Cranes General Design Part3-1: Limit States and proof competence of steel structure.

- ASSEMBLY DRAWINGS

Figure 18.  Holes(X8 Ø 18 H14 ) Drilling position

Figure 19 . Trolley External View Welding Details.

Figure 20 . Trolley Internal View Welding Details.

Figure 21 . Trolley Bottom-Side View Welding Details.

Figure 22 . Trolley Inner Stiffeners Welding Details. (Cross Section View)